Monday

Group 3

- Test aggregate stockpiles

- Develop blends according to super pave specs

- Mix blends and test with constant AC content

- Use blend with air void closest to 4% or ability to get 4%

- Very AC content with blend chosen in step 4(vary content by .5 % for testing )

- Test pucks to determine which AC content meets 4% air voids

- If none meet 4% air voids , iterate to determine mix design with 4% air voids

- If unable to meet 4% air voids, return to step 2

- Test mix  design again to make sure N max is at least 2%

- Choose final mix design